## Slide 1: Metallic Glass
tong
2014-12-19

## Slide 2: Introduction
Metals are made of metallic elements via metallic bonding with long-range translational order.
Glasses involve covalent and ionic bonds, or van der Waals interaction, and are characterized by an amorphous structure without long-range structural correlation.
In 1960s, the first MGs (Au75Si25) were synthesized, overlapping these two categories of materials.

## Slide 3: Introduction: formation and classification
Glasses are essentially ‘‘frozen’’ liquids made by quenching of their high temperature melts.
The first MG sample was obtained at cooling rates 105-106K/s

## Slide 4: Introduction: formation and classification
ΔG VS Viscosity(η)
Not for MGS

## Slide 5: Structure characterization of metallic glasses
Pair distribution function
Structure factor

## Slide 6: Structure characterization of metallic glasses
Coordination Number

## Slide 7: Structure characterization of metallic glasses
Common Neighbor Analysis

## Slide 8: Structure characterization of metallic glasses
Chemical Short-range Order

## Slide 9: Structure characterization of metallic glasses
Bond Angle Distribution

## Slide 10: Structure characterization of metallic glasses
Voronoi Tessellation

## Slide 11: Computational Methods
Reverse Monte Carlo modeling (RMC)

## Slide 12: Computational Methods
Molecular dynamic simulation (MD)

## Slide 13: Computational Methods
Quantum Molecular dynamic simulation (MD)

## Slide 14: Atomic-level structure of metallic galsses
Structure of monatomic liquids
Dense random packing of hard spheres (DRPHS model)

## Slide 15: Atomic-level structure of metallic galsses
Structure of monatomic liquids

## Slide 16: Atomic-level structure of metallic galsses
Structure of Cu-Zr binary metallic glasses

## Slide 17: Atomic-level structure of metallic galsses
Structure of Cu-Zr binary metallic glasses

## Slide 18: Atomic-level structure of metallic galsses
Structure of Cu-Zr binary metallic glasses

## Slide 19: Atomic-level structure of metallic galsses
Structure of Cu-Zr binary metallic glasses

## Slide 20: Atomic-level structure of metallic galsses
Structure of Cu-Zr binary metallic glasses

## Slide 21: Atomic-level structure of metallic galsses
Structure of Cu-Zr binary metallic glasses

## Slide 22: Atomic-level structure of metallic galsses
Structure of Cu-Zr binary metallic glasses

## Slide 23: Atomic-level structure of metallic galsses
Structure of Cu-Zr binary metallic glasses

## Slide 24: Atomic-level structure of metallic galsses
Structure of Cu-Zr binary metallic glasses

## Slide 25: Atomic-level structure of metallic galsses
Structure of Cu-Zr binary metallic glasses

## Slide 26: Atomic-level structure of metallic galsses
Structure of Cu-Zr binary metallic glasses

## Slide 27: Atomic-level structure of metallic galsses
Structure of Cu-Zr binary metallic glasses